## Slide 1: Investigation of Surface Composition and Topography of REBCO Superconducting Tape using Auger Electron Spectroscopy
This work was financially supported by the U.S. Department of Energy, Office and High Energy Physics, award DE-FG02-13ER42036, and benefited from the support of the Materials Science & Engineering Center at UW-Eau Claire. The authors thank SuperPower, Inc. for providing the samples under investigation.
Introduction
Acknowledgements
Initial Steps & Identification
Tanner Olson1, Brynn Dallmann1, Chris Hopp1, Yifei Zhang2, Matthew Jewell1
1Materials Science & Engineering Program  University of Wisconsin – Eau Claire
2SuperPower, Inc.  Schenectady, NY
Celebration of Excellence in Research and Creative Activity (CERCA) April 30-May 4, 2018
The authors thank the UWEC Office of Research and Sponsored Programs for student support at CERCA 2018
UW-Eau Claire
YBa2Cu3O7 (YBCO) is a rare-earth based superconductor that is fabricated as a composite tape. The material has a critical temp. of 93 K, and with the composite structure it can reach up to 400A at 77K, self field.
Under certain conditions the composite tape can delaminate, either at an interface or within a layer.
  The goal of this study is to analyze and quantify the damage present in peel-tested samples, in order to learn more about the nature of delamination initiation and propagation to increase the effectiveness and resiliency of this material.
Morphology
Conclusion
Surface Coverage & Auger
LaMnO3 (LMO)
MgO (Homo)
MgO (IBAD)
Y2O3
Al2O3
The structure of the tape includes a nickel-based Hastelloy substrate for mechanical strength, 5 buffer stacks (as detailed above) to provide epitaxial crystal growth of the YBCO, a silver capping layer for mechanical protection, and a copper layer for electrical stability.
The samples being used in this study have been peel-tested by SuperPower. This leaves us with two halves of the composite tape, which we are then able to analyze. Our first priority was to identify the different layers in the samples in order to gain an understanding of how the delaminations occur. Using a combination of imaging (SEM and laser confocal microscopy) and chemical identification (EDS supplemented with Auger), we were able to successfully identify all layers in our samples.
At high magnification and with complementary Auger analysis, we determined that the yellow striations in the YBCO area are not actually a buffer layer as previously thought, but instead a thin layer of retained YBCO. In this case the delamination occurred within the YBCO layer rather than at an interface.
MgO (IBAD & Homo)
YBCO
LaMnO3
Y2O3
Y2O3
Al2O3
Sample 1
Above are two confocal images taken from our samples. The boxes indicate two different morphology types that are present. The blue boxes indicate ‘narrow’ ridges, which have a more sporadic shape and have a narrower width compared to the other ridge type: ‘wide’ ridges. These have a much more regular, repeatable shape and are shown by the green boxes on the images above.
From these images, we are then able to map the surface in 3D using the laser confocal microscope. Here we show a wide ridge and the associated width and height of the ridges. Through other measurement tools (such as image analysis in Photoshop), we were able to verify this data with similar results.
narrow
wide
Chart: Length (µm)
Sample 1
Chart: Wide and Narrow Ridge Width
Wide Width | 76.8985 | 79.203 | 0 | 79.0416 | 79.8356 | 79.564 | 75.547 | 0 | 0
Wide Average | 78.3316 | 78.3316
Narrow Average | 62.0594 | 62.0594
Narrow Width | 70.085 | 64.957 | 61.325 | 67.164 | 53.691 | 56.239 | 67.038 | 61.416
wide
narrow
Shown to the left is the graph of our data. The error bars show the confidence value range. Both wide and narrow ridge types show consistency across our samples; we can therefore state that the bimodal distribution is similar and comparable across all of our samples.
YBCO composite tape typically delaminates within the superconductor layer in a bimodal fashion (narrow and wide)
Among samples that delaminated within the REBCO layer, there exists a second bimodal trend of narrow and wide coverage in which higher peel strength is correlated with a higher wide ridge coverage percent
Future work:
Collect data from our Auger technique to determine layer dimensions
  Use this information to relate back and improve the YBCO samples
Use this data to form relations linking breakage morphology to sample strength
Since we have verified that the ridge types represent a bimodal distribution and are comparable across our different samples, we can now quantify the area of our samples covered by each ridge type (using Photoshop to manually add an overlay to the capture images). The data shown from this process indicates a second bimodal distribution across our samples in which they possess a 60%/40% wide/narrow coverage or 0%/100% coverage.
Sample 1
wide
narrow
% Coverage | n | Wide % | Narrow % | Verify
Sample 1 | 2 | 60.4 | 39.6 | 100.0
Sample 3 | X | 0.0 | 100.0 | 100.0
Sample 4 | 3 | 62.5 | 37.5 | 100.0
Sample 6 | 3 | 62.4 | 37.6 | 100.0
Sample 7 | 3 | 65.3 | 34.7 | 100.0
Sample 8 | X | 0.0 | 100.0 | 100.0
Sample 9 | X | 0.0 | 100.0 | 100.0
concludes that samples with the 60%/40% coverage are stronger than their 0%/100% counterparts.
Currently, we are using the Auger Electron
Spectroscopy to further analyze newer
samples and determine the depth of
buffer layers that have been experimentally
varied. This process is known as a sputter
and we can compliment this with an
elemental depth graph (as shown here).
These values we can relate back to the peel testing strength for our supplied samples. Although our sample provider does not want us disclosing the actual values of the peel test, we can state that Sample 3 is weaker than Sample 4 by a factor of 3. This